PHYSICAL PHARMACEUTICS II BP(403T) UNIT IV (MICROMERITICS)

CLASS 31

Topic:Methods to determine particle size

# Sedimentation

- The particle size in the subsieve range can be obtained by gravity sedimentation as expressed in Stokes's law,

or

- v is the rate of settling, h is the distance of fall in time t,

- dst is the mean diameter of the particles based on the velocity of sedimentation,

- ρs is the density of the particles and ρ0 that of the dispersion medium,

- g is the acceleration due to gravity,

- η0 is the viscosity of the medium.

- The equation holds exactly only for spheres falling freely without hindrance and at a constant rate.

- The law is applicable to irregularly shaped particles of various sizes as long as that the diameter obtained is a relative particle size equivalent to that of sphere falling at the same velocity as that of the particles under consideration.

- The particles must not be aggregated or clumped together in the suspension because such clumps would fall more rapidly than the individual particles and erroneous results would be obtained.

- The proper deflocculating agent must be found for each sample that will keep the particles free and separate as they fall through the medium.

- For Stokes's law to apply, a further requirement is that the flow of dispersion medium around the particle as it sediments is laminar or streamline.

- In other words, the rate of sedimentation of a particle must not be so rapid that turbulence is set up, because this in turn will affect the sedimentation of the particle

- Whether the flow is turbulent or laminar is indicated by the dimensionless Reynolds number, Re, which is defined as

- Where the symbols have the same meaning as in equation (18-5). Stokes's law cannot be used if Re is greater than 0.2 because turbulence appears at this value.

- On this basis, the limiting particle size under a given set of conditions can be calculated as follows.

- Rearranging equation (18-7) and combining it with equation (18-5) gives

- Under a given set of density and viscosity conditions, equation (18-9)allows calculation of the maximum particle diameter whose sedimentation will be governed by Stokes's law, that is, when Re does not exceed 0.2.

- Several methods based on sedimentation are used. Principal among these are the pipette method, the balance method, and the hydrometer method.

- The Andreasen apparatus, It usually consists of a 550 mL vessel containing a 10 mL pipette sealed into a ground-glass stopper.

- When the pipette is in place in the cylinder, its lower tip is 20 cm below the surface of the suspension.

- The analysis is carried out in the following manner. A 1% or 2% suspension of the particles in a medium containing a suitable deflocculating agent is introduced into the vessel and brought to the 550 mL mark.

- The stoppered vessel is shaken to distribute the particles uniformly throughout the suspension, and the apparatus, with pipette in place, is clamped securely in a constant-temperature bath.

- At various time intervals, 10 mL samples are withdrawn and discharged by means of the two-way stopcock.

# Andreasen apparatus

- As the size of the particles is not uniform the particles settle at different time intervals.

- The larger particles settle at a faster rate and fall below the tip of the pipet tip sooner than smaller particles

- The size distribution and concentration of particles vary along the length of the suspension as sedimentation occurs.

- thus each sample drawn has a lower concentration and contains particles of less size compared to previous sample

- The samples are evaporated and weighed or analyzed by other appropriate means, correcting for the deflocculating agent that has been added.

- The particle diameter corresponding to the various time periods is calculated from Stokes's law, with h in equation being the height of the liquid above the lower end of the pipette at the time each sample is removed.

- The residue or dried sample obtained at a particular time is the weight fraction having particles of sizes less than the size obtained by the Stokes-law calculation for that time period of settling.

- The weight of each sample residue is therefore called the weight undersize, and the sum of the successive weights is known as the cumulative weight undersize. It can be expressed directly in weight units or as percentage of the total weight of the final sediment.

- The cumulative percentage by weight undersize can then be plotted on a probability scale against the particle diameter on a log scale, and the statistical diameters can be obtained

# Advantages

- Ease of analysis

- Accurate technique

- Economy is less

# Representation of data by sedimentation technique:

| Time | Height (cm) | Weight residue units | Strokes diameter(dst) | %of initial suspension |
| --- | --- | --- | --- | --- |

# Particle Volume Measurement-coulter counter technique

- Instrument for measuring the volume of particles is the Coulter counter.

- This instrument operates on the principle that when a particle suspended in a conducting liquid passes through a small orifice on either side of which are electrodes, a change in electric resistance occurs.

- A known volume of a dilute suspension is pumped through the orifice.

- Provided the suspension is sufficiently dilute, the particles pass through essentially one at a time.

- A constant voltage is applied across the electrodes to produce a current.

- As the particle travels through the orifice, it displaces its own volume of electrolyte, and this results in an increased resistance between the two electrodes.

- The change in resistance, which is related to the particle volume, causes a voltage pulse that is amplified and fed to a pulse-height analyzer calibrated in terms of particle size.

- The instrument records electronically all those particles producing pulses that are within two threshold values of the analyzer.

- By systematically varying the threshold settings and counting the number of particles in a constant sample size, it is possible to obtain a particle-size distributionThe instrument is capable of counting particles at the rate of approximately 4000 per second, and so both gross counts and particle size distributions are obtained in a relatively short period of time.

- The data may be readily converted from a volume distribution to a weight distribution.

- The Coulter counter has been used to advantage in the pharmaceutical sciences to study particle growth and dissolution and the effect of antibacterial agents on the growth of microorganisms.

- Particle counting of milled and micronized drugs. Samples of spectinomycin hydrochloride and a micronized steroid were subjected to particle-size analysis together

with polystyrene spheres of 2.0 to 80.0 μm diameter, which were used to calibrate the apparatus.

- The powders showed log-normal distributions and were well characterized by geometric volume mean diameters and geometric standard deviations.

- Accurate particle sizes were obtained between 2 and 80 μm diameter with a precision of about 0.5 μm.

# Advantages

- Results expressed in terms of particle volume from which it is simple to calculate diameter of sphere of equivalent volume

- Instrument can operate with particles between 0.5 and 1000µm

- Operation is very rapid

- Since a large number of particles are to be counted the results are more reliable

- Operational simplicity of the method reduces operator variables enabling reproducible results to be obtained.

# Applications:

- Coulter counter analyzer along with digital computer measures size of spectinomycin hydrochloride (2.0-8.0µm)

- Quality control of pharmaceutical powders

- Used to study mineral part of human kidney stones and to determine critical size range

- Used	for	submicron	size	determination	which	is	used	in	analysis	of microemulsions,pigments and dyes, colloids,micelles and solubilised systems

# Coulter counter

| No of particles counted | Pulse height | Particle size |
| --- | --- | --- |